## Slide 1
CMOS Variable-Gain Low-Noise Amplifier Adopting Transformer-Based Noise Cancelling Technique for 5G NR FR2 Applications
Segyeong Kim and Junhyeop Kim and Junghwan Han
Department of Radio and Information Communication Engineering, Chungnam National University
The chip fabrication and EDA tool were supported by the IC Design Education Center(IDEC), Korea.
This research unveils a novel CMOS variable-gain low-noise amplifier (VGLNA) tailored for the RF range 2 of fifth-generation new radio communication. The technique relies on sophisticated noise-canceling techniques based on transformers to effectively improve performance. Gain control is ingeniously achieved by merging main and current-steering signals through a transformer load with a coupling coefficient below unity. Moreover, The design also mitigates noise from the cascode device in low-gain mode, improving noise performance that has been worsening as VGLNA gain decreases. Fabricated using a 65-nm CMOS process, the implemented VGLNA exhibits gains ranging from 12.1 to 2.7 dB and noise figures from 3.55 to 4.3 dB at 28 GHz. With a nominal supply of 1 V, the design consumes a bias current of 10.6 mA
In this work, a fully integrated CMOS VGLNA design with an innovative transformer-based noise cancellation technique is presented and comprehensively analyzed. The disadvantage that the noise of the main cascode stage increases rapidly as the gain decreases in conventional current steering structures is overcome by introducing a transformer shared by the main cascode stage and the steering stage to eliminate noise in the reverse phase. With this technique, only a total of 0.75 dB noise variation was observed over all gain control ranges, which is an improvement over conventional structures, and a smooth gain control range of 9.4 dB was achieved. Perfectly suited to the requirements of evolving multi-element phased array receiver solutions in the 5G NR domain, this VGLNA implementation offers the possibility of compact and cost-effective designs.
Proposed Transformer-Based Noise Cancelling Technique
Proposed Variable-Gain
Low-Noise Amplifier
Proposed Noise Cancelling Transformer
Calculated results of gain and NF with transformer applied
Proposed Noise Cancelling VGA with Transformer
Proposed transformer layout & Simulation results of the implemented design
+
Measurement Results
- Adding inductors for interstage matching
Simulation results for changing the coupling factor of a transformer
Process | VDD (V) | Area () | Power (mW) | Freq (GHz) | GCR (dB) | Gain (dB) | NF (dB) | S11 (dB) | IB –IIP3 (dB) | IB –P1dB(dB)
65-nm | 1 | 0.13 | 10.6 | 25.7 -29 | 9.4 | 12.1-2.7 | 3.6-4.3 | <-10 | >-6.2 | >-20.5
Process | VDD (V) |  | Power (mW) | Freq (GHz) | GCR (dB) | Gain (dB) | NF (dB) | S11 (dB) | IB –IIP3 (dB) | IB –P1dB(dB)
65-nm | 1 | 0.13 | 10.6 | 25.7 -29 | 9.4 | 12.1-2.7 | 3.6-4.3 | <-10 | >-6.2 | >-20.5
Proposed Noise Cancelling VGA with Transformer
< Measured gains with
different gain settings>
< Measured NFs with
different gain settings>
RF and Analog integrated Circuit dEsign (RF-ACE) Lab, Chungnam National University
Address: 99 Daehak-ro, Bldg E2 Room #425, Yuseong-gu, Daejeon, Korea (34134)
Email: jh.han@cnu.ac.kr Tel: +82-42-821-5665
RF-ACE Lab.